| EASIPRENE |  | Technical Data Sheet |
| --- | --- | --- |
| Thermoplastic Elastomer (TPR) |

| EASIPRENE DB80385 |
| --- |
| Product Description |
|  | EASIPRENE ia a series of SBS (styrene-butadiene-styrene) or SEBS (Styrene-Ethylene-Butadiene-Styrene) type Thermoplastic Rubbers (Elastomers) that combine the properties of vulcanized rubber with the processing advantages of conventional thermoplastics. In other words, they allow the production of rubber-like articles using the fast processing equipment developed by the thermoplastics industries. |
| Processing Method | Other Information |
|  | Extrusion, Injection Molding |  | MetEN71-3；FDA 21CFR177.2600 aq. test |
| General Properties |  |  |  |
| Properties Method Values Type SBS Colour Visual Natural |
| Mechanical Properties |  |  |  |
| Properties Method Values Hardness（5 sec delay） Shore A D2240 80 Density D792 0.97 Elongation @Break % D412 – Die C 321.8 Tensile Strenght MPa D412 – Die C 10.87 100% Modulus MPa D412 – Die C 7.26 300% Modulus MPa D412 – Die C 10.67 Melt Flow Rate @5Kg/190oC g/10min D1238 33.9 |
| Molding Properties |  |  |  |
| Molding Temperature oC Rear 150 - 180 oC Front 160 - 190 oC Nozzle 170 - 190 Mold Temperature oC 25 - 40 Molding Parameters speed medium kPa Boost Pressure 3500 - 5000 kPa Back Pressure 350 - 3000 Cooling Time Sec. 15-30 Drying Time and Temperature No |
| Issue Date: | March 2, 2006 |
|  |  | The properties shown are typical values and for are references only. The value should not be considered as limits to the specification. Since the conditions under which this material is used, are beyond our control, all suggestions and recommendations are without guarantee. |
|  | 梓金（香港）有限公司 Zhi Jin (Hong Kong) Company Limited |