>
> For Elastollan S60A (TPU), we would recommend the following drying 
> process:
>
> Drying Temp.:  80 to 90 Deg. C, (let's keep </= 90 Deg.C since TPU is 
> temp.
>               sensitive)
> Drying Time :  3 to 4 hours (longer hour is preferred for humid climate 
> now).

Processing temp.: 170 - 190 Deg. C,

> Drying temp.    : 90 - 100 Deg. C (for the high humid weather now, but

> these

> high temp. could affect your black master batch with insufficient

> temperature

> resistant, TPU based black master batch is preferred since TPU offered

> higher

> heat resistant).

> Mould temp.     : cooling required when mould temp. exceeds 60 Deg. C that

> resulted in too long the cooling / cycle time.

>